Specifier:  The purpose of this guide specification is to assist the specifier in correctly specifying EXACOR™ subflooring products and its installation.  The specifier needs to edit the guide specification to fit the needs of specific projects.  Contact Huber Engineered Woods to assist in appropriate product selections.  Throughout the guide specification, there are Specifier Notes to assist in the editing of the file. Red text in brackets indicates a selection needs to be made by the design professional.

EXACOR subfloor panels are intended to be used in place of plywood, OSB, or cement-based subflooring, and can minimize the need for a wet-laid gypsum cement underlayment for interior flooring applications. EXACOR can be used in fire resistant assemblies and floor/ceiling assemblies to meet STC/IIC requirements.

SECTION 06 16 23

SUBFLOORING

(Huber Engineered Woods – EXACOR™ Subflooring)

      - SECTION INCLUDES

        - Magnesium Oxide (MgO) Panels for use as structural subflooring.

      - ACTION SUBMITTALS

        - Product Data:  For each type of subflooring product.  Include manufacturer’s technical data indicating performance properties.

        - Shop Drawings:  Indicating location and extent of subflooring [and assemblies].  Include details of joints, corners, and penetrations.

      - INFORMATIONAL SUBMITTALS

        - Evaluation Reports:  From ICC NTA for subflooring products.

        - Product Certifications:  From manufacturer, indicating that subflooring products comply with indicated Performance Criteria.

        - Warranty:  Sample unexecuted copy of manufacturer warranty.

      - CLOSEOUT SUBMITTALS

        - Warranty:  Executed copy of manufacturer warranty.

      - DELIVERY, STORAGE, AND HANDLING

        - Comply with manufacturer's written instructions for storage prior to installation.

          - Store panels horizontally and fully supported.

      - WARRANTY

        - Manufacturer's Warranty:  Manufacturer's standard form in which subflooring manufacturer agrees to repair or replace products that demonstrate deterioration or failure under normal use due to manufacturing defects within warranty period, when installed according to manufacturer's instructions.

          - Warranty Period for Subflooring Products: 10-years from date of manufacture.

- PRODUCTS

      - PERFORMANCE REQUIREMENTS

Specifier: EXACOR Subfloor panels, as a product, are Fire-Resistant and can be used as a component of a tested Fire-Resistant Assembly.  A similar assembly can be used to meet or exceed STC/IIC requirements for dwelling separation.    Contact Huber Engineered Woods to obtain a current list of tested assemblies or refer to EXACOR Fire and Sound Assemblies handbook for assemblies that include finished floor options with STC, IIC and HIIC values.

Fire Resistance Assembly and Sound Rating information is for example only, coordinate project specific requirements, and coordinate with other specification sections to include each assembly component.   Include graphic assembly in drawings.

        - Fire Resistance Assembly in accordance with UL263 Design No L601

          - Rating:  1-Hour Fire Resistant Assembly

        - Bare Sound Rating:

          - STC: 56

          - IIC: 41

          - HIIC: 40

        - Structural Design Values

Specifier: To achieve maximum allowable uniform loading values, panels are required to span two or more joists.

          - Maximum Allowable Uniform Loading (satisfies L/360 LL and L/240 TL deflection – 3 span condition.  Panel long dimension perpendicular to floor framing and edges supported by framing.

            - Joist/Truss spacing 16 inches on center maximum:  100 psf LL/ 120 psf TL

Specifier: Diaphragm values are for wind-controlled designs and do not apply to seismic controlled projects.  Refer to Subfloor Installation Manual for design assembly components required to meet allowable diaphragm capacity

          - Maximum Allowable Diaphragm Capacity for Lateral Load Applied Parallel to Framing (unblocked):  363 plf (ASD) / 579 plf (LRFD)

          - Maximum Allowable Diaphragm Capacity for Lateral Load Applied Perpendicular to Framing (unblocked):  321 plf (ASD) / 512 plf (LRFD)

      - BASIS OF DESIGN

        - EXACOR™ Subfloor by Huber Engineered Woods LLC, Charlotte NC; Phone: (800) 933-9220; Website: www.EXACOR.com.

      - MAGNESIUM OXIDE SUBFLOOR

        - Physical Characteristics

          - Thickness: 3/4-inch (20mm) nominal

          - Panel Size:  48 by 96 inches (1220 by 2440mm) nominal

          - Edge profile:  [Tongue and Groove]

        - Fire-Resistant Characteristics in accordance with ASTM E84 - Standard Test Method for Surface Burning Characteristics of Building Materials

Specifier: Tested in accordance with ASTM E84, subfloor panels exceed the minimum requirements.  First options (0) are the EXACOR test result, second options (≤10/≤5) is the maximum allowable to be classified as Fire-Resistant.  Select the desired value for specific project.

          - Flame Spread: [Less than or equal to 10]

          - Smoke Developed: [Less than or equal to 5]

        - Water Vapor Permeable:

Specifier: Tested in accordance with ASTM E96 for both Method B and Method A for Vapor Permeance and both exceed the minimum requirements.  Select the desired value or test method for specific project.

          - ASTM E96 – Standard Test Methods for Water Vapor Transmission

            - [Greater than or equal to 13 perms according to ASTM E96 Method B]

            - [Greater than or equal to 5 perms accord to ASTM E96 Method A]

        - Mold Resistance:  No mold growth observed in accordance with ASTM G21 – Standard Practice for Determining Resistance of Synthetic Polymeric Materials to Fungi.

      - FASTENERS

Specifier: Review local building code requirements for fastener size and spacing.   EXACOR subflooring is fastened to the framing using BOTH adhesive and mechanical fasteners.

        - Fasteners, General:  Size and type complying with manufacturer's written instructions for Project conditions and requirements of authorities having jurisdiction.

        - Nails:

          - Deformed shank nails with shank diameter of 0.113 inches

          - Minimum #6 by 2 inch (50.8 mm)

          - Corrosion Resistant: Class D, ASTM A153 Hot-Dipped Galvanized or better

          - Conform with ICC-ES AC116 - Acceptance Criteria for Nails and Spikes and ICC-ES AC201 Acceptance Criteria for Staples

        - Screws:

          - Minimum #8 by 2 inch  (50.8 mm)

          - Corrosion Resistant: Class D, ASTM A153 Hot-Dipped Galvanized or better

          - ICC-ES ESR-1539 - Power Driven Staples and Nails for Use in Engineered and Non-Engineered Connections or ICC-ES NER-272 - Power Driven Staples and Nails for Use in All Types of Building Construction

        - Adhesive:

          - Polyurethane or solvent-based

          - Panel manufacturer and adhesive manufacturer recommended for indicated use

          - Conforms with ASTM D3498 - Standard Specification for Adhesives for Field-Gluing Structural Panels to Wood Based Floor System Framing [and] [or] APA AFG-01 - Adhesives for Field-Gluing Plywood to Wood Framing.

- EXECUTION

      - EXAMINATION

        - Examine framing spacing and alignment to determine if work is ready to receive subflooring.  Proceed with subflooring work once conditions meet requirements.

          - Confirm flatness is within tolerances required for flooring.

      - MAGNESIUM OXIDE BOARD SUBFLOORING INSTALLATION

        - Subfloor Installation, General:

          - Install subflooring in accordance with manufacturer's written instructions, requirements of applicable [Evaluation Reports;] [Fire-Resistant Assembly;] [Sound rated assembly], and requirements of authorities having jurisdiction.

          - Maintain designed expansion joints through underlayment.  Do not bridge designed expansion joints in structural panel subfloor.

          - Coordinate termite and decay protection when EXACOR subfloor to be installed within 8 inches of exposed earth.

        - Installation:

Specifier: EXACOR subflooring requires attachment by adhesive and mechanical fasteners to be installed correctly.

          - [Glue and nail] [Glue and screw] to wood framing

          - Mechanical Fastening Pattern:

            - Edges:  6 inches on center max.

            - Field of panel:  12 inches on center max.

            - Place fasteners no closer than ½ inch to the edge

            - Place fastener no closer to the corner than 2 inches.

            - Fastener penetration:

Specifier: Maintain the desired mechanical fastener.

              - [Screws to penetrate framing member 1 inch minimum.]

              - [Nails to penetrate framing members 1.25 inch minimum]

          - Do not bridge expansion joints

          - Long direction of panels to span a minimum of three joists, short end to be supported over framing.

          - Butt panel edges together.  Stagger end joints of adjacent panel runs.

      - PROTECTION AND REPAIR

        - Protect exposed board surfaces from damage due to high construction traffic and concentrated loads during construction.

        - Patch small gaps (less than 2 sq inches) and divots in underlayment with elastomeric patching compound

        - Where large repairs are required, cut out damaged area and replace with piece of underlayment, installing in same manner as initial installation.  Apply patching compound to transition between board and patch.

      - PREPARATION OF FINISH FLOOR COVERINGS

Specifier: Floor flatness requirements may vary depending on type of flooring.  Identify project specific requirements for flooring materials and include in each finish section affected by Underlayment Section.  Wording of this Preparation Article can be included in each associated finish Section.

        - Remove dust, dirt, and debris from underlayment surface.  Ensure panel surface is free from water, oil, grease, and other contaminants.

        - Verify underlayment mechanical fasteners are flush with panel face or slightly below.

        - Identify and correct imperfections in the surface and repair damage as indicated above.

        - Proceed with specific finish preparation prior to installation of flooring finish.

- END OF SECTION

DISCLAIMER: 

This Specification have been written as an aid to the professionally qualified Specifier and Design Professional. The use of this Guide requires the sole professional judgment and expertise of the qualified Specifier and Design Professional to adapt the information to the specific needs for the Building Owner and the Project, to coordinate with their Construction Document Process, and to meet all the applicable building codes, regulations, and laws. HUBER ENGINEERED WOODS EXPRESSLY DISCLAIMS ANY WARRANTY, EXPRESSED OR IMPLIED, INCLUDING THE WARRANTY OF MERCHANTABILITY OR FITNESS FOR PARTICULAR PURPOSE OF THIS PRODUCT FOR THE PROJECT.